Chapter 12(8) Single charge transport in graphene

Dong Su Lee

Soft Innovative Materials Research Center, Korea Institute of Science and Technology (KIST),

Eunha-ri San 101, Bongdong-eup, Wanju-gun, Jeollabuk-do 565-905, South Korea

Email: d.s.lee@kisr.re.kr

Tel: +82 63 219 8145

Fax: +82 63 219 8129

Keywords: graphene, single charge tunneling, quantum dots, single electron transistors, quantum Hall effect, localization, compressible quantum dots

Abstract

The chapter describes single charge tunneling behaviour in graphene devices. Coulomb blockade phenomena observed in graphene constrictions, patterned single electron transistors and graphene nanoribbons are compared with those observed in the conventinal single electron transistors with metallic islands. This chapter also ranges over phenomena when compressible quantum dots are formed in graphene in quantum Hall regime such as mesoscopic conductance fluctuations due to single charge tunneling into/out of the quantum dots.

12.1 Introduction

Generally, in electronic devices, the discreteness of electrons cannot be seen in a macroscopic transport measurement. In other words, behaviors of individual electrons are hidden in an averaged view so that one can measure only statistical observables. Ways to disclose the behaviors of individual charges in transport are related to quantum states in which the wavefunctions of particles are bound, for example induced by i) Coulomb repulsion in a metallic island, i.e. single electron transistors (SETs), ii) quantum confinement due to the size effect, i.e. quantum dots (QDs), and iii) occupation of charges in incompressible condensates at high magnetic fields, i.e. quantum Hall effect (QHE). The investigation of the former two requires small devices in nanometer scale, but the last quantum Hall effect (Klitzing et al., 1980) can be observed in macroscopic devices even over hundreds of micrometers. Interestingly, as recent studies demonstrated, the physics behind the quantum Hall localization is in the same principle as that of SETs or QDs (Ilani et al., 2004). The single charge behaviors have been explored mainly in systems with massive particles, conventional metals and semiconductors. After graphene has been brought into practical realization by mechanical exfoliation form crystalline graphite, this two-dimensional system with massless particles has aroused the interest of the studies on single massless charge transport behaviors.

As an overview, in Section 12.2, an introduction about single charge tunneling behavior will be given. In Section 12.3, Electrical properties of graphene will be discussed. A review of studies on single charge transport behaviors of massless particles in graphene will be given in Section 12.4. Quantum Hall localization behaviors in graphene will be discussed, in particular, with respect to Coulomb blockade physics governing the charge tunneling into the compressible QDs in Section 12.5.

# 12.2 Single charge tunneling

## 12.2.1 Single charge tunneling and Coulomb blockade

Figure 1: A schematic drawing of a single electron transistor (a) and its equivalent circuit (b).

When electrons’ pathways in a conducting channel are blocked by an insulating gap with a capacitance of C, the conduction through the gap occurs by quantum tunneling if the tunneling resistance of the insulating barrier RT is sufficiently larger than the resistance quantum of h/e2 ≈ 25.813 kΩ, where h is the Planck’s constant and e is the electron’s charge. A charging energy scale (Ec  e2/C) plays an important role in the conduction through the barrier in the regime where the thermal energy kBT is much smaller than Ec. Here, kB is the Boltzmann constant and T the temperature. Therefore, single charge tunneling occurs at low temperatures. A common device used to study such single charge tunneling behavior is single electron transistor (SET), which is composed of a metallic “island” and three electrodes of source, drain and gate. See Figure 1(a). These are the same components as those in conventional transistors. The island is completely isolated from the outer environment except for the weak couplings with the three electrodes.

Figure 2: (a, b) A schematic diagram of a single charge tunneling behavior in an SET. When the chemical potentials of the source and drain electrodes lie in the gap between the levels of Ne electrons and (Ne + 1) electrons, conduction is blocked (a). When the level aligns with Fermi energies of source and drain electrons can tunnel one at a time (b). (c) Coulomb oscillation of G as a function of Vg.

In order to inject one additional electron into the island, e.g. from Ne to (Ne + 1), where Ne is the number of electrons occupied the states in the island, an additional energy is required due to the Coulomb repulsion, which amounts the difference of  electrochemical potentials for (Ne + 1) and for Ne electrons, ΔEadd = μN+1 - μN. Here, the electrochemical potential reads as (Beenakker, 1991, Grabert and Devoret, 1992),

.                                                                                           (1)

The gate influence factor is defined as g  Cg/CΣ, where the total capacitance CΣ = Cs + Cd + Cg and Cs, Cd, and Cg are the capacitances of source, drain, and gate, respectively. When the size of the island is small enough, the discrete energy states emerge as the level spacing exceeds the thermal broadening.  The island is then considered as an artificial atom or a quantum dot (QD) and the single-particle energy of the N electrons in the QD, EN, cannot be ignored according to Pauli’s exclusion principle. The energy required for charge injection into the QD equals to the sum of interaction-induced energy (charging energy) and the single-particle energy spacing (frequently termed as quantum confinement); ΔN = εN+1 – εN, where εN is the single-particle energy, ΔEadd = Ec + ΔN. As the electrochemical potential of the island is tuned by modulation of the gate voltage Vg with a small source-drain bias Vds, the discrete energy levels in the island gradually shift up or down. When the chemical potentials of the source and drain electrodes (μs ≈ μd) are placed in the region of the gap between the discrete levels of the island, electrons cannot tunnel from the drain to the island due to the strong Coulomb repulsion. This case is as illustrated in Figure 2(a). Only when a level of the island lies near μs and μd, current can flow as shown in Figure 2(b). The behavior is called as Coulomb Blockade and it leads to an oscillation in the conductance as a function of gate voltage. See Figure 2(c). The tunneling of electrons occurs one at a time because the (Ne + 1) state can be occupied by one electron due to the Pauli’s exclusion principle. This is why the Coulomb blockade behavior is considered as a manifestation of the single charge tunneling. The conduction occurs via the single charge tunneling. The Coulomb peaks are broadened by thermal energy kBT. The relation between the oscillation period ΔVg and the required energy for the single charge tunneling ΔEadd is, egΔVg = ΔEadd  ΔN . If the island size is large enough and the quantum confinement is negligible, the equation can be simplified as egΔVg = ΔEadd. It now shows the definition of the gate influence factor, ratio of total energy of the system to the single electron charging energy of the gate e ΔVg.

## 12.2.2 Coulomb diamonds

Figure 3: Coulomb diamond structures. Gray diamonds are the regions where the conductance is suppressed.

The Coulomb oscillation is also affected by changing the source-drain bias voltage. The energy change after one electron tunnels from the source electrode to the island (ΔEs) and from the island to the drain electrodes (ΔEd) with a finite Vds is,

,                                                             (2)

.                                                          (3)

Details of the calculation can be found in references (Grabert and Devoret, 1992, Beenakker, 1991). Electrons can tunnel from source to drain when both the energies are negative assuming zero temperature, ΔEs < 0 and ΔEd < 0, and otherwise the conductance is zero. This leads to a condition in which the conductance is blocked regime, which is,

,

.                                                              (4)

When projected in a VgVds plane this condition defines a regime where the conduction is prohibited, and regime shows diamond like structures, so-called Coulomb diamonds. Conductance of a SET measured as a function of Vg and Vds is zero in this regime and shows Coulomb peaks at the diamond edges. From the positive and negative slopes of the edges Cd and Cs values can be estimated according to Equation 3.

# 12.3 Electrical properties of graphene

## 12.3.1 Electronic structure of graphene

Figure 4: (a) Atomic structure of graphene. Gray diamond shows the unit cell of the lattice. A and B denote sublattices. (b, c) Band structure of graphene. White hexagon denotes the first Brillouin zone in (b). The three-dimensional image shows both the conduction and valence bands, which touch at K and K’ points.

Graphene is the basic building block of graphite and carbon-based nanomaterials such as carbon nanotubes. It is a purely two-dimensional system since it is composed of a single-layer of carbon atoms which make the honeycomb lattice. It shows unconventional properties such as high thermal conductivity (Balandin et al., 2008), high and nearly equal mobilities at room temperature for both electron and hole conduction up to 200,000 cm2V−1s−1 (Bolotin et al., 2008, Morozov et al., 2008, Dean et al., 2010), and ballistic transport in micrometer length scale (Bolotin et al., 2008, Morozov et al., 2008, Dean et al., 2010). These properties stem from the massless nature of the charge carriers due to the linear energy dispersion relation (Novoselov et al., 2005, Zhang et al., 2005, Wallace, 1947, Castro Neto et al., 2009) and make graphene a promising candidate for nanoelectronic devices.

The lattice structure of graphene as well as its band structure is shown in Figure 4(a). The lattice possesses two sub-lattices denoted by A and B, and they give a rise to the valley degeneracy (or often termed as pseudospin) in addition to the trivial spin degeneracy. Near the Dirac point chirality is defined in regard to this pseudospin associated with the two components of the wave function (Castro Neto et al., 2009). Ignoring the second order hopping, the energy dispersion relation is calculated as,

,                                    (4)

where kx, ky are the components of two-dimensional momentum, 1 is the nearest-neighbor hopping energy and a is the lattice constant, , where a0 is the C-C distance of the graphene honeycomb lattice (Wallace, 1947, Castro Neto et al., 2009). The band structure is shown in Figure 4(b, c). A simplified form of the dispersion relation near zero energy is, E(q) ≈ ±vFq, where vF is the Fermi velocity (~ 1  108 cm/s) and q is the relative moment to Dirac points (K or K’). This linear dispersion is depicted in Figure 4(c). Due to this linear dispersion relation near zero energy the charge carriers follow the Dirac equation rather than Schrödinger equation. The Dirac equation is given by , where is the Pauli matrix and  is the particle’s wavefunction.

## 12.3.2 Transport properties of graphene

Figure 5: Density of states as a function of energy D(E) for particles with linear and quadratic dispersion.

Transport measurement usually deals with low energies. In transport measurements on graphene linear dispersion relation therefore holds. In conventional semiconductors, particles follow a parabolic band, and the density of states (DOS) stays constant regardless of energy. However, in graphene with linear band, the DOS increases linearly with increasing the absolute value of energy (Figure 5). The conduction and valence bands touch each other only at the Dirac points and thus Fermi surface vanishes at zero energy. Despite the zero DOS, there is no band gap at zero energy.

Figure 6: Transfer characteristics measured on a patterned CVD graphene, a graphene flake exfoliated from HOPG, and a suspended graphene device before and after current annealing. Insets show the representative images of the devices (an SEM image on the top and optical microscopy images. The density inhomogeneity obtained from the full width of half maximum of each peak is 1.8  1012, 5  1011, 1.7  1011, and 6  1010 cm-2, for the patterned CVD graphene, the exfoliated HOPG graphene, the suspended graphene and the suspended graphene after annealing, respectively.

The behavior of DOS can be observed via transport measurement on graphene transistors. The upper inset of Figure 6 shows a scanning tunneling microscope image of the suspended graphene device. The lower two insets of Figure 6 show optical images of the device exfoliated from highly oriented pyrolytic graphite (HOPG) and transferred onto a Si substrate  (left-hand side ) and the device grown on a metal substrate and transferred onto Si (right-hand side). The Si chips are covered by a thermally grown oxide layer with a thickness of around 300 nm. The oxide layer makes monolayer graphene visible (Blake et al., 2007) as well as acting as a gate dielectric. The highly doped Si is used as a backgate to modulate the charge carrier density (n) in graphene. For the 300 nm thick SiO2, the carrier density can be estimated by the relation: n = Vbg, where the gate efficiency factor  ≈ 7.2  1010 cm-2V-1 (Novoselov et al., 2004). Figure 6(d) shows the resistance (R) as a function of the backgate voltage (Vbg), which is often referred to as transfer characteristics. Due to the vanishing DOS near the “charge neutral point”, a resistance peak appears. The roughly symmetric transfer curves demonstrate the electron-hole symmetry.

Figure 7: Schematic drawing of a disordered potential landscape. Light (dark) gray indicates the regions with excess holes (electrons).

Here one should note that the charge neutrality point does not necessarily correspond to the Dirac point of the band. The explanation is as follows. One cannot expect a system without disorder in nature. The origin of disorder in graphene can be structural defects (Hashimoto et al., 2004, Gass et al., 2008, Meyer et al., 2008b, Warner et al., 2009), charged impurities(Ando, 2006, Chen et al., 2008, Ni et al., 2010), corrugation (Geringer et al., 2009, Locatelli et al., 2010), ripples (Bao et al., 2009), substrate roughness (Ishigami et al., 2007), etc., or a combination of these. Regardless of their origin, disorders induce a potential variation along the sample as seen in Figure 7. Following the disordered potential landscape, the local band structure varies. As a consequence of the disordered potential and the gapless nature of the graphene band, when the Fermi energy (EF) is near charge neutral point, both regions where the charge carriers are dominated by electrons and by holes appear. This is a unique phenomenon of graphene, the so-called electron-hole puddles formation (Martin et al., 2008) whereas density puddles with either positive or negative charges only are observed in conventional semiconductor 2DESs. Due to the electron-hole puddles one may expect a very high resistance near the charge neutral point. However, the puddle edges do not produce a clear boundary condition because the charges are not totally bound in a single puddle due to Klein tunneling (Katsnelson et al., 2006, Cheianov and Fal’ko, 2006). As a result, a finite resistance peak appears. The full-width-at-half maximum (fwhm) of the peak in an Rn curve is a rough estimation of the density inhomogeneity (Δnd). In Figure 6, graphene grown by chemical vapor deposition (CVD) shows much larger disordered density (Δnd  1.8  1012 cm-2) than exfoliated graphene from highly oriented pyrolytic graphite (HOPG) (Δnd  5  1011 cm-2). Because the substrate roughness or embedded charges inside the SiO2 substrate are the main source of the disorder in graphene transistors (Martin et al., 2008), when the substrate is removed and graphene device is suspended (Du et al., 2009, Bolotin et al., 2009), the resistance peak becomes very narrow showing low Δnd  6  1010 cm-2. Also, the resistance at the peak becomes higher as seen in Figure 6.

Figure 8: Typical quantum Hall behavior of graphene. Longitudinal resistance (Rxx) and Hall resistance (Rxy) traces measured at 12 T are plotted as a function of Vg - VN, where VN is the voltage of charge neutrality.

When a magnetic field is applied, the quantum Hall effect (QHE) is observed in graphene as in conventional 2DESs. However, the behavior is distinct from that of 2DESs. Conventional 2DESs have massive carriers following a parabolic band structure and as a result exhibits quantum Hall plateaus at integer filling factors (integer QHE). Graphene having the linear dispersion relation and the zero band gap, however, shows quantum Hall plateaus at Hall conductivities xy = e2/h for the filling factor sequence  = ±2, ±6, ±10, , ignoring interactions, which is the so-called “half integer QHE” (Zhang et al., 2005, Novoselov et al., 2005). Here h is the Planck’s constant. Note that the four-fold degeneracy with spin and valley symmetries is taken into account. The QHE in graphene is shown in Figure 8. The unique half integer QHE is due to the zero energy Landau level (LL) degeneracy. The LL energy in graphene is given by EN = ±ħωc(N + 1/2), where ħ is the Planck’s constant over 2, ωc = eB/m∗ is the cyclotron frequency and N is the quantum number. Here, B is the magnetic field and m∗ is the effective mass. The DOS at zero magnetic field collapse into LLs at a finite magnetic field. The LL degeneracy is 4eB/h. The factor 4 arises from the four-fold degeneracy. However, in the lowest LL pinned at zero energy, which is by itself unusual, electrons and holes share the state and both are half degenerate. When disorder becomes weaker other more fragile QH states induced by interactions emerge. For instance spontaneous symmetry breaking gives rise to the states with two-fold symmetry (spin or pseudospin) at  = 0, ±4, ±8, , as well as the fully broken symmetry states at ν = ±1, ±3,  (Zhang et al., 2006, Goerbig et al., 2006, Gusynin et al., 2008, Yang, 2007, Checkelsky et al., 2008, Jung and MacDonald, 2009). Also fractional quantum Hall states appear as a result of the formation of composite quasi-particles (Tőke and Jain, 2007, Papic et al., 2009, Du et al., 2009, Bolotin et al., 2009, Dean et al., 2011).

# 12.4 Single charge tunneling in graphene

When electrons in graphene are confined in one-dimension (graphene nanoribbons) or in two-dimension (graphene quantum dots), single charge tunneling behavior occurs within the massless Dirac nature of particles. This will promise rich physics behind the confined Dirac particles. For the study the advantages of graphene over other nanomaterials such as carbon nanotubes (CNTs) or semiconductor nanowires are its two-dimensionality and the fact that it can be patterned by a lithographic process followed by etching. Such process is easily accessible because it is based on the conventional top-down approach. The quantum confinement effect in graphene nanoribbons and in graphene single electron transistors has been investigated in experiments as well as in theoretical studies. They will be reviewed in this section.

## 12.4.1 Band gap opening in graphene

One of the most attractive electronic applications of graphene is field effect transistors since it exhibits excellent electrical properties such as very high carrier mobility with an electron-hole symmetry (Novoselov et al., 2004, Novoselov et al., 2005, Geim and Novoselov, 2007, Semenoff, 1984) and ballistic transport in a large length scale of microns (Miao et al., 2007). Moreover, it shows a high thermal conductivity which exceeds those of diamond and graphite (Seol et al., 2010) so that it may be used for integrated devices with a much lower heat dissipation compared to the conventional silicon-based devices. However, we have a serious problem that graphene has only a zero-band gap. The off-state current is not totally suppressed near the charge neutral point. This is because there are always charge carriers near charge neutral point, electron-hole puddles, due to the presence of disorders. Martin et al. have well demonstrated this localized phenomena of the electron-hole puddles in graphene (Martin et al., 2008).

Opening a band gap in graphene is therefore one of the key issues in the quest to achieve a high performance of graphene electronic devices. Several ways to open a band gap in graphene have been proposed; graphene superlattices, biased bilayer graphene and graphene nanoribbons. The approach of graphene superlattices is to break the valley symmetry by introducing another periodicity in addition to the honeycomb lattice. There have been suggestions to produce these graphene superlattices, e.g. the periodic ripples often found in graphene grown on metal substrates (Guinea and Low, 2010), anti-dot lattices (Furst et al., 2009, Pedersen et al., 2008, Liu et al., 2009), a periodic potential (Tiwari and Stroud, 2009), patterned hydrogen adsorption (Balog et al., 2010), substrate-induced superlattice on BN (Giovannetti et al., 2007), lithographic patterning (Martinazzo et al., 2010, Meyer et al., 2008a), etc. An energy gap feasible for the field effect devices, say, more than 0.1 eV, has been achieved in biased bilayer graphene. In order to induce an asymmetry of the on-site energies in the top and bottom layers (McCann, 2006, Min et al., 2007, Castro et al., 2007), researchers have used molecular doping on graphene grown by thermal decomposition of SiC (Ohta et al., 2006), a dual-gate structure fabricated on an exfoliated bilayer graphene flake (Zhang et al., 2009, Oostinga et al., 2008, Xia et al., 2010, Taychatanapat and Jarillo-Herrero, 2010) or dual molecular doping on both the top and the bottom of a bilayer graphene flake (Park et al., 2012).

## 12.4.2 Graphene nanoribbons

Figure 9: The atomic structures of an armchair nanoribbon (Na = 11) (a) and a zigzag ribbon (Nz = 7) (b). Dark gray and light gray dots indicate the sublattices. The edge sites are indicated by the thick lines.

Another approach for the band gap opening is to spatially confine the electron wave functions in graphene. For instance, one can shrink the width of a graphene field effect device in the nanometer scale which results in graphene nanoribbons. They show metallic or semiconducting behaviors depending on their width and atomic structure at the edge. This is analogous to carbon nanotubes, where the boundary condition is determined by the rolling direction (chiral vector) of a graphene sheet while in graphene nanoribbons two edges determine the boundary condition. Graphene nanoribbons have been intensively studied as another route toward the field effect transistor application (Lemme et al., 2007, Lin et al., 2008, Meric et al., 2008, Liao et al., 2010, Li et al., 2009, Kedzierski et al., 2009, Lin et al., 2010, Kedzierski et al., 2008, Moon et al., 2009, Yang et al., 2012) because they exhibit a tunable band gap. Graphene nanoribbons serve not only as the high performance field effect transistors but also, in the respect of quantum mechanics, as a system for a fundamental study on single charge tunneling behavior, in particular that of massless Dirac particles. When a nanoribbon or a nanoconstriction interconnects two metallic systems (either metal electrodes or bulk graphene flakes), the energy gap (or the different energy gaps distributed along the translational direction) of the constriction acts as a tunnel barrier which is essential for the single charge tunneling.

Figure 10: Band structures of armchair (a) and zigzag ribbons (b) of various widths calculated by a tight binding model. The image was modified figures from (Nakada et al., 1996).

The electronic structure of the graphene nanoribbons (Fujita et al., 1996, Nakada et al., 1996, Wakabayashi et al., 1999, Ezawa, 2006) was theoretically studied much earlier (in 1996) than the exfoliation of the one-atom-thick sheet, “graphene” (in 2004) (Novoselov et al., 2004). The basic electronic properties of graphene nanoribbons were even then discovered by calculations using a tight binding model. Fujita et al. (Fujita et al., 1996) showed the band strucures of graphene nanoribbons with zigzag edges and armchair edges. Here, they found that for graphene with zigzag edges, a peculiar edge ferromagnetizm is present with an antiparallel spin orientation between the two opposite edges and for graphene with armchair edges, a band gap appears. Nakada et al. (Nakada et al., 1996)  and Esawa (Ezawa, 2006) revealed that graphene nanoribbon with armchair edges has an energy gap Δ that is tunable by changing the width w. Here, w usually scales in the units of the number of dimer lines perpendicular to the translational direction of the ribbon, Na and Nz for the graphene nanoribbons with armchair edges and with zigzag edges, respectively (See Figure 9). Depending on the boundary conditions, if some of the one-dimensional modes cross the Dirac point, and then the ribbon shows metallic behavior, but it is otherwise semiconducting with a finite energy gap. When Na = 3p or 3p + 1, graphene with armchair edges shows a band gap while it is metallic when Na = 3p + 2, where p is an positive integer. Nanoribbons with the zigzag edge on the other hand always exhibit a flat band at zero energy regardless of the ribbon width as shown in Figure 10. However, according to a recent ab initio calculation by (Son et al., 2006), even for graphene nanoribbons with zigzag edges, gaps appear because of a staggered sublattice potential on the hexagonal lattice due to edge magnetization (See Figure 11).

Figure 11: Band structure of a Na = 12 zigzag graphene nanoribbon. z0 and z1 are the direct band gap and the energy splitting at kdz = , respectively. The data was taken from (Son et al., 2006).

Figure 12: Atomic force microscope (a) and scanning electron microscope images (b, c) of graphene nanoribbon devices. (d-f) Temperature dependent conductance of the ribbons with various widths. (g) The energy gap as a function of the width of devices. The image is modified from figures in (Han et al., 2007).

It is not yet possible to experimentally fabricate a graphene nanoribbons with clear edges either of armchair or of zigzag orientation only. The edges are usually rough containing both the armchair and ziazag orientations not only in patterned nanoribbons but also in exfoliated flakes. See, for instance (Krauss et al., 2010). There are several ways to fabricate graphene nanoribbons. A common approach is to reduce the size of graphene by e-beam lithography and a plasma etching technique (Han et al., 2007, Chen et al., 2007, Todd et al., 2008). For this approach, graphene is often obtained by mechanical exfoliation from crystals of natural graphite or HOPG using a sticky tape (Novoselov et al., 2004), and deposited on a silicon substrate with an about 300 nm thick thermally grown oxide, which make monolayer graphene visible in an optical microscope due to an increased optical path and the notable opacity of graphene (Blake et al., 2007). The transferred flakes are indentified by an optical microscope. An e-beam resist is spin-coated on the SiO2 substrate with the transferred graphene flakes. An appropriate etching pattern is drawn on the resist on top of graphene flakes by e-beam lithography, and the exposed resist pattern is developed by a chemical solvent. Now, a part of the graphene flake is exposed and the chip is subjected to a reactive ion etching (RIE) chamber for the O2 or Ar plasma etching of the part. After removal of the resist, the patterned graphene nanoribbons or nanoconstrictions are prepared, and the electrical contacts to the devices are made by further processes of e-beam lithography and metalization. The energy gap in graphene nanoribbons shows a inversely proportional behavior to the width of the ribbons (Han et al., 2007), who found that Δ [eV] ≈ 0.2/(w[nm] – 16[nm]). The energy gap for instance 0.1 eV can be obtained in graphene nanoribbon with w ~ 18 nm, say, less than 20 nm. Though the procedure is quite common and reliable, it is not suitable for definition of atomically-clear edge structures due to the anisotropic nature of plasma etching process and a bad etch selectivity of graphene to the resist mask under the plasma.

Figure 13: (a) Conductance as a function of Vg. (b) A smoothed trace of the curve in (a). (c) Stability diagram of a graphene nanoribbon device. (d) Zoom of the plot in (c). Image is modified from the figures in (Molitor et al., 2009).

Although coherent transport is expected through a graphene nanoribbon (Muñoz-Rojas et al., 2006, Darancet et al., 2009), it is not yet possible to fabricate clear edges on graphene nanoribbons. Instead, at low temperatures, the gate dependent behavior conductance (G) is often cluttered by oscillations or fluctuations (Molitor et al., 2009, Terres et al., 2011, Tombros et al., 2011). They may be due to the network of graphene quantum dots (QDs) and/or the rough edge structures. Even Coulomb diamond-like structures are quite commonly observed in graphene nanoribbons (Molitor et al., 2009, Terres et al., 2011, Safron et al., 2011). However, nanoribbons with the disordered edge (mixture of zigzag and armchair edges) have shown the conductance quantization sequence of the integer multiples of 2e2/h  due to the ballistic charges of graphene and and the valley degeneracy lifting (Tombros et al., 2011, Brey and Fertig, 2006).

Figure 14: Graphene nanoribbons fabricated by anisotropic etching. The image is modified from a figure in (Yang et al., 2010).

A more promising way to control the edge is based on the carbo-thermal reduction of SiO2 to SiO in argon environment at around 700 °C (Nemes-Incze et al., 2010). The carbon atoms at the edge of graphene are used for the process and the flake edges aligned in the crystallographic direction. A Raman spectroscopy study confirmed the graphene edge orientaions (Krauss et al., 2010). A similar result was obtained by a hydrogen plasma etching (Xie et al., 2010), a gas-phase chemistry etching process (Wang and Dai, 2010) or by plasma etching using nanospheres as a mask (Liu et al., 2011). In these method, long graphene nanoribbon transistors with controlled edges were fabricated (Lu et al., 2010, Liu et al., 2011, Yang et al., 2010, Wang and Dai, 2010, Xie et al., 2010). However, single charge tunneling behavior using the edge-controlled nanoribbons or constrictions has not yet been reported.

## 12.4.3 Graphene single electron transistors

Graphene SETs can be defined by isolating a part of a graphene flake and connecting it with two constrictions (or nanoribbons) on the opposite sides, which serve as the source and drain capacitors. A side gate structure can be patterned on graphene or Si backgate can also be used to modulate the electrostatic energy of the island. So far, in order to pattern the SET structure on graphene researchers often used the plasma etching technique. The basic structure of graphene SETs is the same as conventional SETs based on metals or semiconductors. However, there is a clear distinction. Due to the massless nature of the charges in the system the quantum confinement is different from that for conventional SETs, where the charges obey the massive parabolic dispersion relation.

Figure 15: Separation of nearest-neighbor peaks at zero bias voltage (Vg) measured in a graphene quantum dot. The peak spacing shows a large variation (a factor of 5 or more). Image was taken from (Ponomarenko et al., 2008).

Figure 16: Source-drain current as a function of the gate voltage and Coulomb diamond structures. Image taken from (Stampfer et al., 2008).

Here we consider the quantum confinement energy which becomes important when the size of the island is small enough, i.e. it is considered as a QD. For massive carriers for instance in 2DES, the quantum confinement energy of an island is given from the two-dimensional box problem by ΔN ≈ h2/(8med2), where me is the effective mass and d is the diameter of the island. It shows ΔN is proportional to 1/d2. However, a different spectrum is applied for graphene SETs with massless charge carriers as, ΔN ≈ vFh/(2d). Here ΔN is inversely proportional to d. The 1/d dependence of the quantum confinement energy for a graphene SET has been demonstrated by (Ponomarenko et al., 2008). They have also found that the oscillation period ΔVg varies randomly (not showing even-odd sequence due to the spin degeneracy of the massive carriers) and the variation of the chaotic (ΔVg) is larger than typical variations observed in non-graphene QDs by orders of magnitude (See Figure 15). Furthermore, (ΔVg) becomes notably broader with decreasing d approximately following (ΔVg)   1/d2. Such a “Dirac billiard” behavior raises the importance of the shape of the graphene QD for the behavior of the single charge tunneling in the system. According to a theoretical calculation (Bardarson et al., 2009), a regular-shaped (disc) graphene QDs show sharp resonances which reduces the effective gated region but the irregular-shaped (stadium) QDs cannot support bound states due to a chaotic dynamics. Irregular Coulomb oscillation has been observed by others in a normal SET structure with patterned island (Schnez et al., 2009) and Coulomb oscillation behaviors in nanoconstrictions (Terres et al., 2011, Droscher et al., 2011). More studies are needed since a regular ΔVg has also been observed in a normal SETs (Stampfer et al., 2008, Guettinger et al., 2008) or in a direct measurement on compressible QDs in quantum Hall regime using scanning tunneling microscopy (STM), where they observed the four-fold periodicity due to the spin and valley degeneracies (Jung et al., 2011). In addition to the ground state Coulomb diamonds, the excited states  and phenomena in a double QD system have also been revealed in experiments (Schnez et al., 2009, Liu et al., 2010, Molitor et al., 2010). Despite the intensive studies, the interesting physics behind the confined massless particles are largely unexplored. For instance, it would be an intriguing experiment if one fabricates the SET with the edge-controlled constrictions using the crystallographic etching or even with a hexagonal-shaped graphene island as described in Section 8.4.1.  Also, controlled spin states using specific edges will provide an insight for a spin qbits where a long-distance coupling is possible (Trauzettel et al., 2007).

# 12.5 Charge localization in graphene

## 12.5.1 Localization in quantum Hall regime

Figure 17: Schematics of the compressible QD formation at high magnetic field.

Localization of charges in quantum Hall regime, which gives rise to the quantum Hall plateaus, has been found to occur within the boundaries of Coulomb blockade physics (Ilani et al., 2004, Martin et al., 2009). For the charge confinement, the insulating barriers of incompressible strips play an important role. As shown in Section 8.3.2, a disordered potential landscape in graphene induces a density profile along the sample. The carriers are redistributed to flatten the disordered potential as shown in Figure 17. This linear screening is not valid when a perpendicular magnetic field is applied though. In some regions, the level degeneracy is completely filled as n increases and the carriers cannot screen out the disordered potential in these regions. Due to the gap between the LLs, carriers can no longer be injected into there, i.e. the regions become totally incompressible. The incompressible regions serve as insulating barriers to enclose the compressible dots. The charges coming into the compressible QDs are governed by Coulomb blockade physics. Every charging event occurs by one electron (or hole) at a time into the discrete levels of the QDs. This leads to a sudden jump in the local compressibility (dn/d), where  is the chemical potential. At higher B field, the same density profile appears at accordingly higher n since the LL degeneracy is proportional to B (eB/h). The compressibility spikes produce lines parallel to specific filling factors as shown in Figure 17. The presence of the compressible QDs in the QH regime has been demonstrated by a direct transport measurement on the dots using an STM tip (Jung et al., 2011).

## 12.5.2 Compressible quantum dots in quantum Hall regime

Figure 18: Conductance (a) and transconductance (b) curves measured at B = 15 T. Diagrams show the measurement schematics. Images taken from (Lee et al., 2012).

The influence of the compressible QDs on macroscopic conductance of graphene device has recently been investigated by magnetotransport measurements of conductance fluctuations (Lee et al., 2012). Conductance curves as a function of Vbg at high magnetic fields often possess fluctuations, which clutter the main conductance quantization behavior. However, these fluctuations are found to be a manifestation of charge localization. Although the local process is not shown in mesoscopic transport due to the averaging the fluctuations can reflect the single charge tunneling that occurs locally into the compressible QDs. Conductance as a function of n at 15 T is shown in Figure 18(a). In addition to the quantized steps and the signatures of quantization, there are fluctuations, which are reproducible for repeated measurements. These fluctuations are more pronounced if one measures transconductance gm. Here, an ac modulation δVbg is applied to the backgate, only the ac component of the source-drain current δIds is measured, and gm = δIds / δVbg. Both measurements were done with a dc-voltage bias of Vds = 500 V. The frequency of δVbg was 433 Hz and its root-meansquare amplitude was 10 mV. Insets show the schematics of the measurements.

Figure 19: (a) Greyscale rendition of gm in the (n, B)-plane. (b),(c) Correlation function C() for the data in the windows which is marked in the rendition. Image is taken from (Lee et al., 2012).

The same backgate sweep was repeated for different magnetic fields. The result is plotted in a color rendition in a (n, B)-plane. See Figure 19(a). There are many line features and they are classified into groups in which lines are parallel to each other. The lines in a group run parallel to a certain filling factor line. The lines parallel to ν = ±2 are the most strong and sharp as the filling factor 2 is most profound because of the largest gap between N = 0 and N = 1 LLs. Also, ν = 6-line can be discerned which is another half integer filling factor. Surprisingly, more fragile broken symmetry states and fractional quantum Hall states can be clearly seen in the fluctuation map while such states are invisible or only seen as faint signatures if visible. Details can be found in (Lee et al., 2012).

Figure 20: Schematic illustration of compressible quantum dots and edge channels in a graphene device.

The color rendition with the line features resembles the local compressibility map measured on graphene (Martin et al., 2009) as well as earlier on GaAs 2DESs (Ilani et al., 2004) using a scanning SET. Thus, it is natural to associate the conductance fluctuations with the compressible spike lines. Far from the complete filling of the level degeneracy, the linear screening holds. As one increases n by modulation of the backgate, compressible quantum dots emerge as described in Section 8.5.1 Incompressible strips play a role to isolate the dots. As illustrated in Figure 20, conducting channels are always present near the sample edge due to the edge potential. Current can flow through these edge states. During modulation of n, the compressible spikes may emerge for some dots due to the Coulomb blockade allowing charging of the dots. Accordingly, additional transport channels through the network of the dots may be turned on, off or their path is altered. At every compressible spike the charging give rises to a fluctuation of the source-drain current. The same fluctuation behavior would occur at the same deviation of n from complete filling even at a different magnetic field. As a consequence, the conductance fluctuation peaks or valleys run parallel to the filling factor lines in the (n, B)-plane. It should be noted that the line features of the conductance fluctuations have already been discovered in GaAs 2DESs (Cobden et al., 1999) and recently in graphene (Branchaud et al., 2010, Velasco et al., 2010). They just measured the resistance and the results showed only the lines parallel to the single particle states, half integer QH states in graphene and integer QH states in GaAs, respectively. In the transconductance measurement using the lock-in technique reveals the presence of more fragile interaction induced states of broken symmetry states and fractional quantum Hall states (Lee et al., 2012). For instance,  = 0 and  = 1 lines for broken symmetry states and a fractional filling factor (ν = 1/3) lines are also found in the color rendition of Figure 19(a).

Figure 21: Schematic illustration of the data analysis using C().

In order to visualize the strength of the fluctuations lines as well as to determine the filling factor of the lines we transform the data set in a window into a correlation spectrum as a function of filling factor, C(), which shows how much the data along a certain slope in the (n, B)-plane are correlated and thus how distinctively they make the line with the slope. A schematic illustration of the calculation is shown in Figure 21. Here, the data set of gm as a function of n and B can be regarded as a matrix, D(n, B). A data window is chosen in nmin ≤ n ≤ nmax and Bmin ≤ B ≤ Bmax. The matrix element is then, Dij ≡ D(nj, Bi). Here, nj (Bi) is the jth (ith) element of n (B) from nmin (Bmin). The correlation function as a function of filling factor is then defined as,

,                                                                                (5)

where, δν is an allowance function defined as, δν = 1 if r(θm) < ra and δν = 0, otherwise. Here r(θm) is the distance in the unit of data pixels (Δn and ΔB) between the point of Dpq and the line crossing the point of Dkl with a slope, s = tan(π/2 ‒ θm), i.e. the line for the filling factor, ν(θm) = (Φ0/s)·(Δn/ΔB). Here, the denominator in Equation 5 is a normalization factor. The allowance factor is chosen as ra = 1. For the value of ν(θm) parallel to the line features of the gm peaks or deeps the summation of  Dkl Dpq will be larger whereas it will be cancelled out when ν(θm) line is not parallel to the line features in the map. The analysis is shown in Figure 22.

Figure 22: Correlation function. Images taken from (Lee et al., 2012).

In the spectrum of C(ν) obtained from the data in the lower left rectangle in the color rendition of Figure 19, filling factors of  = 2, 4, 6 and 10. Here,  = 4 state is in particular interesting because it is attributed to a symmetry breaking either of spin or valley. Also, it did not appear in the conductance data (Lee et al., 2012). Fractional quantum Hall states appear as well. C(ν) obtained from the data in the upper rectangular window clearly shows the filling factors  = 1/3, 2/3, which are most pronounced fractional quantum Hall states in graphene. They are not seen in conductance measurement.

Figure 23: Gate dependence of dIds = dVds (top) and greyscale rendition of dIds = dVds as a function of Vds and Vg (bottom). Image is taken from (Lee et al., 2012).

The compressible QD scenario described above is valid only when the non-linear screening of the disorder potential produces compressible QDs isolated by the insulating barriers. Despite the recent observation of the single charge tunneling behavior on a compressible QD using STM tip (Jung et al., 2011) a direct transport measurement through the network of QDs is desirable for a better understanding on the influence of the network of QDs to the conductance fluctuations. It is however prohibited by the presence of the edge channel in parallel to the network of QDs. A direct transport measurement on the network of QDs was however possible since the quantum Hall insulating behavior emerges at high magnetic fields. The true insulating behavior originates from the absence of the edge states due to the valley symmetry breaking for the zero energy states (Yang, 2007). The differential conductance, dIds/dVds, as well as a color rendition of it as a function of Vbg and Vds are shown in Figure 23. The stability diagram of the differential conductance exhibits Coulomb diamond structures, which unambiguously proves the existence of the tunnel barriers which isolate the QDs. The estimated length scale of the QDs from the diamond structures in Fig. 3f ranges from 160 to 400 nm, which can be regarded as the disorder length scale since the QDs formation is due to the non-linear screening of the disorder potential. It was estimated from the diamond structures as d2 = 4Cg/(e), where Cg = C/(sp-1 + sn-1), where sp and sn are the positive and negative slopes of diamond structures. The disorder length scale can also be comparable to the mean free path (lmfp) of the system. From the conductivity near the charge neutral point without magnetic field for our suspended sample, 3.5e2/h, we deduce lmfp 350 nm (Mucciolo and Lewenkopf, 2010), which is consistent with the length scale estimated from Coulomb diamonds. The irregularity of the diamonds can be either the result from the network of QDs or the result from the non-disk-like shape of the QDs where the chaotic resonance has been predicted  (Bardarson et al., 2009).

# 12.6 Conclusion

Recent advances in the progress to control the electronic properties of graphene are significant and they promise not only the applications of the electronic devices such as transistors but also of quantum computational devices. However, physics behind the single charge behavior in graphene has not yet been fully uncovered. For instance it is not yet possible to open a band gap of graphene in bulk scale. Attempts for realization of single electron transistors or quantum dots of graphene by the size control were reviewed in Section 8.4.  In addition, it is discussed how the mesoscopic transport is affected by the single charge tunneling and how the localization of individual charges can be captured in macroscopic devices in Section 8.5. The massless particles obeying the linear dispersion relation is the key point to understand the single charge transport in graphene and such understanding in single charge transport will provide an insight toward the future nanoelectronics.

12.7 References

ANDO, T. 2006. Screening effect and impurity scattering in monolayer graphene. Journal of the Physical Society of Japan, 75.

BALANDIN, A. A., GHOSH, S., BAO, W., CALIZO, I., TEWELDEBRHAN, D., MIAO, F. & LAU, C. N. 2008. Superior Thermal Conductivity of Single-Layer Graphene. Nano Letters, 8, 902-907.

BALOG, R., JORGENSEN, B., NILSSON, L., ANDERSEN, M., RIENKS, E., BIANCHI, M., FANETTI, M., LAEGSGAARD, E., BARALDI, A., LIZZIT, S., SLJIVANCANIN, Z., BESENBACHER, F., HAMMER, B., PEDERSEN, T. G., HOFMANN, P. & HORNEKAER, L. 2010. Bandgap opening in graphene induced by patterned hydrogen adsorption. Nat Mater, 9, 315-319.

BAO, W., MIAO, F., CHEN, Z., ZHANG, H., JANG, W., DAMES, C. & LAU, C. N. 2009. Controlled ripple texturing of suspended graphene and ultrathin graphite membranes. Nat Nano, 4, 562-566.

BARDARSON, J. H., TITOV, M. & BROUWER, P. W. 2009. Electrostatic Confinement of Electrons in an Integrable Graphene Quantum Dot. Physical Review Letters, 102, 226803.

BEENAKKER, C. W. J. 1991. THEORY OF COULOMB-BLOCKADE OSCILLATIONS IN THE CONDUCTANCE OF A QUANTUM DOT. Physical Review B, 44, 1646-1656.

BLAKE, P., HILL, E. W., NETO, A. H. C., NOVOSELOV, K. S., JIANG, D., YANG, R., BOOTH, T. J. & GEIM, A. K. 2007. Making graphene visible. Applied Physics Letters, 91.

BOLOTIN, K. I., GHAHARI, F., SHULMAN, M. D., STORMER, H. L. & KIM, P. 2009. Observation of the fractional quantum Hall effect in graphene. Nature, 462, 196-199.

BOLOTIN, K. I., SIKES, K. J., JIANG, Z., KLIMA, M., FUDENBERG, G., HONE, J., KIM, P. & STORMER, H. L. 2008. Ultrahigh electron mobility in suspended graphene. Solid State Communications, 146, 351-355.

BRANCHAUD, S., KAM, A., ZAWADZKI, P., PEETERS, F. M. & SACHRAJDA, A. S. 2010. Transport detection of quantum Hall fluctuations in graphene. Physical Review B, 81, 121406.

BREY, L. & FERTIG, H. A. 2006. Electronic states of graphene nanoribbons studied with the Dirac equation. Physical Review B, 73, 235411.

CASTRO, E. V., NOVOSELOV, K. S., MOROZOV, S. V., PERES, N. M. R., DOS SANTOS, J. M. B. L., NILSSON, J., GUINEA, F., GEIM, A. K. & NETO, A. H. C. 2007. Biased Bilayer Graphene: Semiconductor with a Gap Tunable by the Electric Field Effect. Physical Review Letters, 99, 216802.

CASTRO NETO, A. H., GUINEA, F., PERES, N. M. R., NOVOSELOV, K. S. & GEIM, A. K. 2009. The electronic properties of graphene. Reviews of Modern Physics, 81, 109-162.

CHECKELSKY, J. G., LI, L. & ONG, N. P. 2008. Zero-Energy State in Graphene in a High Magnetic Field. Physical Review Letters, 100, 206801.

CHEIANOV, V. V. & FAL’KO, V. I. 2006. Selective transmission of Dirac electrons and ballistic magnetoresistance of n-p junctions in graphene. Physical Review B, 74, 041403.

CHEN, J. H., JANG, C., ADAM, S., FUHRER, M. S., WILLIAMS, E. D. & ISHIGAMI, M. 2008. Charged-impurity scattering in graphene. Nat Phys, 4, 377-381.

CHEN, Z. H., LIN, Y. M., ROOKS, M. J. & AVOURIS, P. 2007. Graphene nano-ribbon electronics. Physica E-Low-Dimensional Systems & Nanostructures, 40, 228-232.

COBDEN, D. H., BARNES, C. H. W. & FORD, C. J. B. 1999. Fluctuations and Evidence for Charging in the Quantum Hall Effect. Physical Review Letters, 82, 4695-4698.

DARANCET, P., OLEVANO, V. & MAYOU, D. 2009. Coherent Electronic Transport through Graphene Constrictions: Subwavelength Regime and Optical Analogy. Physical Review Letters, 102, 136803.

DEAN, C. R., YOUNG, A. F., CADDEN-ZIMANSKY, P., WANG, L., REN, H., WATANABE, K., TANIGUCHI, T., KIM, P., HONE, J. & SHEPARD, K. L. 2011. Multicomponent fractional quantum Hall effect in graphene. Nat Phys, 7, 693-696.

DEAN, C. R., YOUNG, A. F., MERICI, LEEC, WANGL, SORGENFREIS, WATANABEK, TANIGUCHIT, KIMP, SHEPARD, K. L. & HONEJ 2010. Boron nitride substrates for high-quality graphene electronics. Nat Nano, 5, 722-726.

DROSCHER, S., KNOWLES, H., MEIR, Y., ENSSLIN, K. & IHN, T. 2011. Coulomb gap in graphene nanoribbons. Physical Review B, 84.

DU, X., SKACHKO, I., DUERR, F., LUICAN, A. & ANDREI, E. Y. 2009. Fractional quantum Hall effect and insulating phase of Dirac electrons in graphene. Nature, 462, 192-195.

EZAWA, M. 2006. Peculiar width dependence of the electronic properties of carbon nanoribbons. Physical Review B, 73, 045432.

FUJITA, M., WAKABAYASHI, K., NAKADA, K. & KUSAKABE, K. 1996. Peculiar localized state at zigzag graphite edge. Journal of the Physical Society of Japan, 65, 1920-1923.

FURST, J. A., PEDERSEN, J. G., FLINDT, C., MORTENSEN, N. A., BRANDBYGE, M., PEDERSEN, T. G. & JAUHO, A. P. 2009. Electronic properties of graphene antidot lattices. New Journal of Physics, 11.

GASS, M. H., BANGERT, U., BLELOCH, A. L., WANG, P., NAIR, R. R. & GEIM, A. K. 2008. Free-standing graphene at atomic resolution. Nat Nano, 3, 676-681.

GEIM, A. K. & NOVOSELOV, K. S. 2007. The rise of graphene. Nature Materials, 6, 183-191.

GERINGER, V., LIEBMANN, M., ECHTERMEYER, T., RUNTE, S., SCHMIDT, M., R CKAMP, R., LEMME, M. C. & MORGENSTERN, M. 2009. Intrinsic and extrinsic corrugation of monolayer graphene deposited on SiO_{2}. Physical Review Letters, 102, 076102.

GIOVANNETTI, G., KHOMYAKOV, P. A., BROCKS, G., KELLY, P. J. & VAN DEN BRINK, J. 2007. Substrate-induced band gap in graphene on hexagonal boron nitride: Ab initio density functional calculations. Physical Review B, 76, 073103.

GOERBIG, M. O., MOESSNER, R. & DOU OT, B. 2006. Electron interactions in graphene in a strong magnetic field. Physical Review B, 74, 161407.

GRABERT, H. & DEVORET, M. H. 1992. New York and London, Plenum Press.

GUETTINGER, J., STAMPFER, C., HELLMUELLER, S., MOLITOR, F., IHN, T. & ENSSLIN, K. 2008. Charge detection in graphene quantum dots. Applied Physics Letters, 93.

GUINEA, F. & LOW, T. 2010. Band structure and gaps of triangular graphene superlattices. Philosophical Transactions of the Royal Society a-Mathematical Physical and Engineering Sciences, 368, 5391-5402.

GUSYNIN, V. P., MIRANSKY, V. A., SHARAPOV, S. G. & SHOVKOVY, I. A. 2008. Edge states, mass and spin gaps, and quantum Hall effect in graphene. Physical Review B, 77, 205409.

HAN, M. Y., ÖZYILMAZ, B., ZHANG, Y. & KIM, P. 2007. Energy Band-Gap Engineering of Graphene Nanoribbons. Physical Review Letters, 98, 206805.

HASHIMOTO, A., SUENAGA, K., GLOTER, A., URITA, K. & IIJIMA, S. 2004. Direct evidence for atomic defects in graphene layers. Nature, 430, 870-873.

ILANI, S., MARTIN, J., TEITELBAUM, E., SMET, J. H., MAHALU, D., UMANSKY, V. & YACOBY, A. 2004. The microscopic nature of localization in the quantum Hall effect. Nature, 427, 328-332.

ISHIGAMI, M., CHEN, J. H., CULLEN, W. G., FUHRER, M. S. & WILLIAMS, E. D. 2007. Atomic Structure of Graphene on SiO2. Nano Letters, 7, 1643-1648.

JUNG, J. & MACDONALD, A. H. 2009. Theory of the magnetic-field-induced insulator in neutral graphene sheets. Physical Review B, 80, 235417.

JUNG, S., RUTTER, G. M., KLIMOV, N. N., NEWELL, D. B., CALIZO, I., HIGHT-WALKER, A. R., ZHITENEV, N. B. & STROSCIO, J. A. 2011. Evolution of microscopic localization in graphene in a magnetic field from scattering resonances to quantum dots. Nat Phys, 7, 245-251.

KATSNELSON, M. I., NOVOSELOV, K. S. & GEIM, A. K. 2006. Chiral tunnelling and the Klein paradox in graphene. Nat Phys, 2, 620-625.

KEDZIERSKI, J., HSU, P. L., HEALEY, P., WYATT, P. W., KEAST, C. L., SPRINKLE, M., BERGER, C. & DE HEER, W. A. 2008. Epitaxial graphene transistors on SIC substrates. Ieee Transactions on Electron Devices, 55, 2078-2085.

KEDZIERSKI, J., HSU, P. L., REINA, A., KONG, J., HEALEY, P., WYATT, P. & KEAST, C. 2009. Graphene-on-Insulator Transistors Made Using C on Ni Chemical-Vapor Deposition. Ieee Electron Device Letters, 30, 745-747.

VON KLITZING, K., DORDA, G. & PEPPER, M. 1980. New Method for High-Accuracy Determination of the Fine-Structure Constant Based on Quantized Hall Resistance. Physical Review Letters, 45, 494-497.

KRAUSS, B., NEMES-INCZE, P. T., SKAKALOVA, V., BIRO, L. S. P., VON KLITZING, K. & SMET, J. H. 2010. Raman Scattering at Pure Graphene Zigzag Edges. Nano Letters, 10, 4544-4548.

LEE, D. S., SKAKALOVA, V., WEITZ, R. T., SMET, J. H. & VON KLITZING, K., 2012. Transconductance fluctuations as a probe for interaction-induced quantum Hall states in graphene. Physical Review Letters, 109, 056602.

LEMME, M. C., ECHTERMEYER, T. J., BAUS, M. & KURZ, H. 2007. A graphene field-effect device. Ieee Electron Device Letters, 28, 282-284.

LI, X., CAI, W., AN, J., KIM, S., NAH, J., YANG, D., PINER, R., VELAMAKANNI, A., JUNG, I., TUTUC, E., BANERJEE, S. K., COLOMBO, L. & RUOFF, R. S. 2009. Large-Area Synthesis of High-Quality and Uniform Graphene Films on Copper Foils. Science, 324, 1312-1314.

LIAO, L., BAI, J. W., QU, Y. Q., LIN, Y. C., LI, Y. J., HUANG, Y. & DUAN, X. F. 2010. High-kappa oxide nanoribbons as gate dielectrics for high mobility top-gated graphene transistors. Proceedings of the National Academy of Sciences of the United States of America, 107, 6711-6715.

LIN, Y.-M., DIMITRAKOPOULOS, C., JENKINS, K. A., FARMER, D. B., CHIU, H.-Y., GRILL, A. & AVOURIS, P. 2010. 100-GHz Transistors from Wafer-Scale Epitaxial Graphene. Science, 327, 662.

LIN, Y.-M., JENKINS, K. A., VALDES-GARCIA, A., SMALL, J. P., FARMER, D. B. & AVOURIS, P. 2008. Operation of Graphene Transistors at Gigahertz Frequencies. Nano Letters, 9, 422-426.

LIU, L., ZHANG, Y. L., WANG, W. L., GU, C. Z., BAI, X. D. & WANG, E. G. 2011. Nanosphere Lithography for the Fabrication of Ultranarrow Graphene Nanoribbons and On- Chip Bandgap Tuning of Graphene. Advanced Materials, 23, 1246-+.

LIU, W., WANG, Z. F., SHI, Q. W., YANG, J. & LIU, F. 2009. Band-gap scaling of graphene nanohole superlattices. Physical Review B, 80, 233405.

LIU, X. L., HUG, D. & VANDERSYPEN, L. M. K. 2010. Gate-defined graphene double quantum dot and excited state spectroscopy. Nano Letters, 10, 1623-1627.

LOCATELLI, A., KNOX, K. R., CVETKO, D., MENTEŞ, T. O., NIÑO, M. A., WANG, S., YILMAZ, M. B., KIM, P., OSGOOD, R. M. & MORGANTE, A. 2010. Corrugation in Exfoliated Graphene: An Electron Microscopy and Diffraction Study. Acs Nano, 4, 4879-4889.

LU, Y., GOLDSMITH, B., STRACHAN, D. R., LIM, J. H., LUO, Z. T. & JOHNSON, A. T. C. 2010. High-On/Off-Ratio Graphene Nanoconstriction Field-Effect Transistor. Small, 6, 2748-2754.

MARTIN, J., AKERMAN, N., ULBRICHT, G., LOHMANN, T., SMET, J. H., VON KLITZING, K. & YACOBY, A. 2008. Observation of electron-hole puddles in graphene using a scanning single-electron transistor. Nature Physics, 4, 144-148.

MARTIN, J., AKERMAN, N., ULBRICHT, G., LOHMANN, T., VON KLITZING, K., SMET, J. H. & YACOBY, A. 2009. The nature of localization in graphene under quantum Hall conditions. Nat Phys, 5, 669-674.

MARTINAZZO, R., CASOLO, S. & TANTARDINI, G. F. 2010. Symmetry-induced band-gap opening in graphene superlattices. Physical Review B, 81, 245420.

MCCANN, E. 2006. Asymmetry gap in the electronic band structure of bilayer graphene. Physical Review B, 74, 161403.

MERIC, I., HAN, M. Y., YOUNG, A. F., OZYILMAZ, B., KIM, P. & SHEPARD, K. L. 2008. Current saturation in zero-bandgap, top-gated graphene field-effect transistors. Nat Nano, 3, 654-659.

MEYER, J. C., GIRIT, C. O., CROMMIE, M. F. & ZETTL, A. 2008a. Hydrocarbon lithography on graphene membranes. Applied Physics Letters, 92.

MEYER, J. C., KISIELOWSKI, C., ERNI, R., ROSSELL, M. D., CROMMIE, M. F. & ZETTL, A. 2008b. Direct Imaging of Lattice Atoms and Topological Defects in Graphene Membranes. Nano Letters, 8, 3582-3586.

MIAO, F., WIJERATNE, S., ZHANG, Y., COSKUN, U. C., BAO, W. & LAU, C. N. 2007. Phase-coherent transport in graphene quantum billiards. Science, 317, 1530-1533.

MIN, H., SAHU, B., BANERJEE, S. K. & MACDONALD, A. H. 2007. Ab initio theory of gate induced gaps in graphene bilayers. Physical Review B, 75, 155115.

MOLITOR, F., JACOBSEN, A., STAMPFER, C., G TTINGER, J., IHN, T. & ENSSLIN, K. 2009. Transport gap in side-gated graphene constrictions. Physical Review B, 79, 075426.

MOLITOR, F., KNOWLES, H., DROESCHER, S., GASSER, U., CHOI, T., ROULLEAU, P., GUETTINGER, J., JACOBSEN, A., STAMPFER, C., ENSSLIN, K. & IHN, T. 2010. Observation of excited states in a graphene double quantum dot. Epl, 89.

MOON, J. S., CURTIS, D., HU, M., WONG, D., MCGUIRE, C., CAMPBELL, P. M., JERNIGAN, G., TEDESCO, J. L., VANMIL, B., MYERS-WARD, R., EDDY, C. & GASKILL, D. K. 2009. Epitaxial-Graphene RF Field-Effect Transistors on Si-Face 6H-SiC Substrates. Ieee Electron Device Letters, 30, 650-652.

MOROZOV, S. V., NOVOSELOV, K. S., KATSNELSON, M. I., SCHEDIN, F., ELIAS, D. C., JASZCZAK, J. A. & GEIM, A. K. 2008. Giant Intrinsic Carrier Mobilities in Graphene and Its Bilayer. Physical Review Letters, 100, 016602.

MU OZ-ROJAS, F., JACOB, D., FERN NDEZ-ROSSIER, J. & PALACIOS, J. J. 2006. Coherent transport in graphene nanoconstrictions. Physical Review B, 74, 195417.

MUCCIOLO, E. R. & LEWENKOPF, C. H. 2010. Disorder and electronic transport in graphene. Journal of Physics-Condensed Matter, 22.

NAKADA, K., FUJITA, M., DRESSELHAUS, G. & DRESSELHAUS, M. S. 1996. Edge state in graphene ribbons: Nanometer size effect and edge shape dependence. Physical Review B, 54, 17954-17961.

NEMES-INCZE, P., MAGDA, G., KAMARAS, K. & BIRO, L. P. 2010. Crystallographically selective nanopatterning of graphene on SiO2. Nano Research, 3, 110-116.

NI, Z. H., PONOMARENKO, L. A., NAIR, R. R., YANG, R., ANISSIMOVA, S., GRIGORIEVA, I. V., SCHEDIN, F., BLAKE, P., SHEN, Z. X., HILL, E. H., NOVOSELOV, K. S. & GEIM, A. K. 2010. On Resonant Scatterers As a Factor Limiting Carrier Mobility in Graphene. Nano Letters, 10, 3868-3872.

NOVOSELOV, K. S., GEIM, A. K., MOROZOV, S. V., JIANG, D., KATSNELSON, M. I., GRIGORIEVA, I. V., DUBONOS, S. V. & FIRSOV, A. A. 2005. Two-dimensional gas of massless Dirac fermions in graphene. Nature, 438, 197-200.

NOVOSELOV, K. S., GEIM, A. K., MOROZOV, S. V., JIANG, D., ZHANG, Y., DUBONOS, S. V., GRIGORIEVA, I. V. & FIRSOV, A. A. 2004. Electric Field Effect in Atomically Thin Carbon Films. Science, 306, 666-669.

OHTA, T., BOSTWICK, A., SEYLLER, T., HORN, K. & ROTENBERG, E. 2006. Controlling the Electronic Structure of Bilayer Graphene. Science, 313, 951-954.

OOSTINGA, J. B., HEERSCHE, H. B., LIU, X. L., MORPURGO, A. F. & VANDERSYPEN, L. M. K. 2008. Gate-induced insulating state in bilayer graphene devices. Nature Materials, 7, 151-157.

PAPIC, Z., GOERBIG, M. O. & REGNAULT, N. 2009. Theoretical expectations for a fractional quantum Hall effect in graphene. Solid State Communications, 149, 1056-1060.

PARK, J., JO, S. B., YU, Y.-J., KIM, Y., YANG, J. W., LEE, W. H., KIM, H. H., HONG, B. H., KIM, P., CHO, K. & KIM, K. S. 2012. Single-Gate Bandgap Opening of Bilayer Graphene by Dual Molecular Doping. Advanced Materials, 24, 407-411.

PEDERSEN, T. G., FLINDT, C., PEDERSEN, J., MORTENSEN, N. A., JAUHO, A. P. & PEDERSEN, K. 2008. Graphene antidot lattices: Designed defects and spin qubits. Physical Review Letters, 100.

PONOMARENKO, L. A., SCHEDIN, F., KATSNELSON, M. I., YANG, R., HILL, E. W., NOVOSELOV, K. S. & GEIM, A. K. 2008. Chaotic Dirac Billiard in Graphene Quantum Dots. Science, 320, 356-358.

SAFRON, N. S., BREWER, A. S. & ARNOLD, M. S. 2011. Semiconducting Two-Dimensional Graphene Nanoconstriction Arrays. Small, 7, 492-498.

SCHNEZ, S., MOLITOR, F., STAMPFER, C., GUTTINGER, J., SHORUBALKO, I., IHN, T. & ENSSLIN, K. 2009. Observation of excited states in a graphene quantum dot. Applied Physics Letters, 94.

SEMENOFF, G. W. 1984. Condensed-Matter Simulation of a Three-Dimensional Anomaly. Physical Review Letters, 53, 2449-2452.

SEOL, J. H., JO, I., MOORE, A. L., LINDSAY, L., AITKEN, Z. H., PETTES, M. T., LI, X., YAO, Z., HUANG, R., BROIDO, D., MINGO, N., RUOFF, R. S. & SHI, L. 2010. Two-Dimensional Phonon Transport in Supported Graphene. Science, 328, 213-216.

SON, Y.-W., COHEN, M. L. & LOUIE, S. G. 2006. Energy Gaps in Graphene Nanoribbons. Physical Review Letters, 97, 216803.

STAMPFER, C., SCHURTENBERGER, E., MOLITOR, F., GUETTINGER, J., IHN, T. & ENSSLIN, K. 2008. Tunable graphene single electron transistor. Nano Letters, 8, 2378-2383.

TAYCHATANAPAT, T. & JARILLO-HERRERO, P. 2010. Electronic Transport in Dual-Gated Bilayer Graphene at Large Displacement Fields. Physical Review Letters, 105.

TERRES, B., DAUBER, J., VOLK, C., TRELLENKAMP, S., WICHMANN, U. & STAMPFER, C. 2011. Disorder induced Coulomb gaps in graphene constrictions with different aspect ratios. Applied Physics Letters, 98.

TIWARI, R. P. & STROUD, D. 2009. Tunable band gap in graphene with a noncentrosymmetric superlattice potential. Physical Review B, 79, 205435.

TODD, K., CHOU, H.-T., AMASHA, S. & GOLDHABER-GORDON, D. 2008. Quantum Dot Behavior in Graphene Nanoconstrictions. Nano Letters, 9, 416-421.

TŐKE, C. & JAIN, J. K. 2007. SU(4) composite fermions in graphene: Fractional quantum Hall states without analog in GaAs. Physical Review B, 75, 245440.

TOMBROS, N., VELIGURA, A., JUNESCH, J., GUIMARAES, M. H. D., VERA-MARUN, I. J., JONKMAN, H. T. & VAN WEES, B. J. 2011. Quantized conductance of a suspended graphene nanoconstriction. Nat Phys, 7, 697-700.

TRAUZETTEL, B., BULAEV, D. V., LOSS, D. & BURKARD, G. 2007. Spin qubits in graphene quantum dots. Nature Physics, 3, 192-196.

VELASCO, J., JR., LIU, G., JING, L., KRATZ, P., ZHANG, H., BAO, W., BOCKRATH, M. & LAU, C. N. 2010. Probing charging and localization in the quantum Hall regime by graphene p–n–p junctions. Physical Review B, 81, 121407.

WAKABAYASHI, K., FUJITA, M., AJIKI, H. & SIGRIST, M. 1999. Electronic and magnetic properties of nanographite ribbons. Physical Review B, 59, 8271-8282.

WALLACE, P. R. 1947. The Band Theory of Graphite. Physical Review, 71, 622-634.

WANG, X. & DAI, H. 2010. Etching and narrowing of graphene from the edges. Nature Chem., 2, 661-665.

WARNER, J. H., RUMMELI, M. H., GE, L., GEMMING, T., MONTANARI, B., HARRISON, N. M., BUCHNER, B. & BRIGGS, G. A. D. 2009. Structural transformations in graphene studied with high spatial and temporal resolution. Nat Nano, 4, 500-504.

XIA, F., FARMER, D. B., LIN, Y.-M. & AVOURIS, P. 2010. Graphene Field-Effect Transistors with High On/Off Current Ratio and Large Transport Band Gap at Room Temperature. Nano Letters, 10, 715-718.

XIE, L., JIAO, L. & DAI, H. 2010. Selective Etching of Graphene Edges by Hydrogen Plasma. Journal of the American Chemical Society, 132, 14751-14753.

YANG, H., HEO, J., PARK, S., SONG, H. J., SEO, D. H., BYUN, K.-E., KIM, P., YOO, I., CHUNG, H.-J. & KIM, K. 2012. Graphene Barristor, a Triode Device with a Gate-Controlled Schottky Barrier. Science, 336, 1140-1143.

YANG, K. 2007. Spontaneous symmetry breaking and quantum Hall effect in graphene. Solid State Communications, 143, 27-32.

YANG, R., ZHANG, L. C., WANG, Y., SHI, Z. W., SHI, D. X., GAO, H. J., WANG, E. G. & ZHANG, G. Y. 2010. An Anisotropic Etching Effect in the Graphene Basal Plane. Advanced Materials, 22, 4014-4019.

ZHANG, Y., JIANG, Z., SMALL, J. P., PUREWAL, M. S., TAN, Y. W., FAZLOLLAHI, M., CHUDOW, J. D., JASZCZAK, J. A., STORMER, H. L. & KIM, P. 2006. Landau-Level Splitting in Graphene in High Magnetic Fields. Physical Review Letters, 96, 136806.

ZHANG, Y., TANG, T.-T., GIRIT, C., HAO, Z., MARTIN, M. C., ZETTL, A., CROMMIE, M. F., SHEN, Y. R. & WANG, F. 2009. Direct observation of a widely tunable bandgap in bilayer graphene. Nature, 459, 820-823.

ZHANG, Y. B., TAN, Y. W., STORMER, H. L. & KIM, P. 2005. Experimental observation of the quantum Hall effect and Berry's phase in graphene. Nature, 438, 201-204.